Publication Date 2025

| DXL STEEL FRAMING SYSTEMS PRODUCT DATA SHEET |  |
| --- | --- |

HAT CHANNEL

CEILING CHANNEL

| DXL Hat Channels are cold-formed galvanized steel furring profiles used in ceiling, wall lining and drywall framing systems XL- HC SERIES 1. PRODUCT INFORMATION Product Name; Ceiling Hat Channel. Model No.; DXL-HC Series. Category; Ceiling Framing System. Application; Ceiling and wall furring systems. 2. DIMENSIONS Profile Size (A); Standard＆Custom Sizes. Thickness (T); 0.40 - 0.60 mm. Length; 2800 / 3000 / Custom（≥2000）. 3. MATERIAL Material; Hot-dip Galvanized steel. Zinc Coating; Z100 - Z275 g/m². Surface finish; Galvanized silver-grey finish; custom color powder coating available.. 4. TOLERANCE Thickness; 0/-0.02 mm. Width; 0/-0.5 mm. Length; ±1.0 mm. | 6.Product Photo DXL-WS SERIES. 7.SECTIONVIEW DXL-WS PROFILE. 8. PACKAGING Standard bundle packing category-name printed bag. Easy for storage and identification |
| --- | --- |

Specification Table

| Model | Overall Width | Top Width | Flange Width | Height | Thickness（mm） | Length (T) mm | Packing |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DXL-HC-42 | 42 | 23 | 6 | 7 | 0.40 - 0.60 mm | 2800 3000 custom（≥2000） | As per order confirmation |
| DXL-HC-50 | 50 | 28 | 7 | 10 | 0.40 - 0.60 mm | 2800 3000 custom（≥2000） | As per order confirmation |
| DXL-HC-60 | 60 | 35 | 9 | 12 | 0.40 - 0.60 mm | 2800 3000 custom（≥2000） | As per order confirmation |

Notes

- Custom length available for all models

- Special dimensions and thickness are available upon request

- Theoretical weight is for reference only. Actual weight shall prevail