Publication Date 2025

| DXL STEEL FRAMING SYSTEMS PRODUCT DATA SHEET |  |
| --- | --- |

HAT CHANNEL

CEILING CHANNEL

| DXL- HC SERIES DXL Hat Channels are cold-formed galvanized steel furring profiles used in ceiling, wall lining and drywall framing systems. DXL 帽型龙骨采用优质冷轧镀锌钢板成型，适用于吊顶、墙面找平及石膏板基层系统。 1. PRODUCT INFORMATION / 产品信息 Product Name 产品名称; Ceiling Hat Channel. Model No. 型号; DXL-HC Series. Category 类别; Ceiling Framing System. Application 应用; Ceiling and wall furring systems. 2. DIMENSIONS / 尺寸参数 Profile Size (A); Standard＆Custom Sizes. Thickness (T); 0.4 0.5 0.6. Length; 2800 / 3000 / Custom（≥2000）. 3. MATERIAL / 材料与表面处理 Material材质; Galvanized steel. Zinc Coating 镀锌层; Z100 - Z275 g/m². Surface finish 表面处理; Hot-dip Galvanized. 4. TOLERANCE / 公差标准 Thickness 厚度公差; ±0.03 mm. Width 宽度公差; ±0.50 mm. Length 长度公差; ±5.0 mm. | 6.Product Photo / 产品实物 DXL-WS SERIES. 7.SECTIONVIEW / 截面图 DXL-WS PROFILE. 8. PACKAGING / 包装示意 Standard bundle packing category-name printed bag. Easy for storage and identification |
| --- | --- |

For Sales Inquiries, please contact our global support team via WhatsApp:＋78764422 or dxlmetal@gmail.com

DXL—Reliable Quality，Global Trust

Specification Table

| Model | Overall Width | Top Width | Flange Width | Height | Thickness（mm） | Length (T) mm |
| --- | --- | --- | --- | --- | --- | --- |
| DXL-HC-42 | 42 | 23 | 6 | 7 | 0.35 0.4 0.45 0.5 | 2800 3000 custom（≥2000） |
| DXL-HC-60 | 60 | 35 | 10 | 12 | 0.35 0.4 0.45 0.5 | 2800 3000 custom（≥2000） |
| DXL-HC-70 | 70 | 34 | 10 | 20 | 0.35 0.4 0.45 0.5 | 2800 3000 custom（≥2000） |
| DXL-HC-54 | 54 | 38 | 10 | 16 | 0.35 0.4 0.45 0.5 | 2800 3000 custom（≥2000） |
| DXL- |  |  |  |  |  |  |

Notes

- Custom length available for all models

- Special dimensions and thickness are available upon request

For Sales Inquiries, please contact our global support team via WhatsApp:＋78764422 or dxlmetal@gmail.com

DXL—Reliable Quality，Global Trust