Publication Date 2025

| DXL STEEL FRAMING SYSTEMS PRODUCT DATA SHEET |  |
| --- | --- |

DRYWALL J-BEAD

| XL- JB SERIES DXL J-Beads are galvanized steel edge trim profiles used to finish and protect exposed drywall board edges. 1. PRODUCT INFORMATION Product Name; Drywall F-Bead. Model No.; DXL-JB Series. Category; Drywall Framing System. Application; Drywall edge finishing and termination. 2. DIMENSIONS Profile Size (A); Standard＆Custom Sizes. Thickness (T); 0.35 - 0.50 mm. Length; 2800 / 3000 / Custom（≥2000）. 3. MATERIAL Material; Hot-dip Galvanized steel. Zinc Coating; Z100 - Z275 g/m². Surface finish; Galvanized silver-grey finish; custom color powder coating available.. 4. TOLERANCE Thickness; 0/-0.02 mm. Width; 0/-0.5 mm. Length; ±1.0 mm. | 6.Product Photo DXL-WS SERIES. 7.SECTIONVIEW DXL-WS PROFILE. 8. PACKAGING Standard bundle packing category-name printed bag. Easy for storage and identification |
| --- | --- |

Specification Table

| Model | Vertical Leg | Horizontal Leg | Return Edge | Thickness（T）mm | Length (T) mm | Packing |
| --- | --- | --- | --- | --- | --- | --- |
| DXL-JB-27-20-20 | 27 | 20 | 20 | 0.35 - 0.50 mm | 2800 3000 custom（≥2000） | As per order confirmation |
| DXL-JB-30-21 | 30 | 21 | 21 | 0.35 - 0.50 mm | 2800 3000 custom（≥2000） | As per order confirmation |
| DXL-JB-27-20-12 | 27 | 20 | 17 | 0.35 - 0.50 mm | 2800 3000 custom（≥2000） | As per order confirmation |

Notes

- Custom length available for all models

- Special dimensions and thickness are available upon request

- Theoretical weight is for reference only. Actual weight shall prevail