Publication Date 2025

| DXL STEEL FRAMING SYSTEMS PRODUCT DATA SHEET |  |
| --- | --- |

SQUARE LEG HAT CHANNEL

CEILING SYSTEMS

| DXL- HSC SERIES DXL Square Leg Hat Channels are galvanized steel furring profiles with straight side legs, used for ceiling and wall framing applications. DXL 方腿帽型龙骨采用镀锌钢板成型，两侧为直边结构，适用于吊顶及墙面基层系统。 1. PRODUCT INFORMATION / 产品信息 Product Name 产品名称; Ceiling Square Leg Hat Channel. Model No. 型号; DXL-HSC Series. Category 类别; Ceiling Framing Systems. Application 应用; Ceiling and wall framing systems. 2. DIMENSIONS / 尺寸参数 Profile Size (A); Standard＆Custom Sizes. Thickness (T); 0.5 0.6 0.7 0.8. Length; 2800 / 3000 / Custom（≥2000）. 3. MATERIAL / 材料与表面处理 Material材质; Galvanized steel. Zinc Coating 镀锌层; Z100 - Z275 g/m². Surface finish 表面处理; Hot-dip Galvanized. 4. TOLERANCE / 公差标准 Thickness 厚度公差; ±0.03 mm. Width 宽度公差; ±0.50 mm. Length 长度公差; ±5.0 mm. | 6.Product Photo / 产品实物 DXL-WS SERIES. 7.SECTIONVIEW / 截面图 DXL-WS PROFILE. 8. PACKAGING / 包装示意 Standard bundle packing category-name printed bag. Easy for storage and identification |
| --- | --- |

For Sales Inquiries, please contact our global support team via WhatsApp:＋78764422 or dxlmetal@gmail.com

DXL—Reliable Quality，Global Trust

Specification Table

| Model | Overall Width | Top Width | Flange Width | Height | Thickness （mm） | Length (T) mm |
| --- | --- | --- | --- | --- | --- | --- |
| DXL- | 90 | 50 | 20 | 50 | 0.5 0.6 0.7 0.8 | 2800 3000 custom（≥2000） |
| DXL- | 52 | 32 | 10 | 16 | 0.5 0.6 0.7 0.8 | 2800 3000 custom（≥2000） |
| DXL- |  |  |  |  |  | 2800 3000 custom（≥2000） |
| DXL- |  |  |  |  |  | 2800 3000 custom（≥2000） |
| DXL- |  |  |  |  |  | 2800 3000 custom（≥2000） |

Notes

- Custom length available for all models

- Special dimensions and thickness are available upon request

For Sales Inquiries, please contact our global support team via WhatsApp:＋78764422 or dxlmetal@gmail.com

DXL—Reliable Quality，Global Trust