Publication Date 2025

| DXL STEEL FRAMING SYSTEMS PRODUCT DATA SHEET |  |
| --- | --- |

DRYWALL STUD

| DXL-WS-SERIES DXL Drywall Studs are cold-formed steel sections used in non-load bearing drywall framing systems. 1. PRODUCT INFORMATION Product Name; Drywall Stud. Model No.; DXL-WS Series. Category; Drywall Framing System. Application; Interior Partition Walls. 2. DIMENSIONS Web Width (A); 64 73 92 100 150 mm. Thickness (T); 0.40 - 0.60 mm. Length; 2800 / 3000 / Custom（≥2000）. 3. MATERIAL Material; Hot-dip Galvanized steel. Zinc Coating; Z100 - Z275 g/m². Surface finish; Galvanized silver-grey finish; custom color powder coating available.. 4. TOLERANCE Thickness; 0/-0.02 mm. Width; 0/-0.5 mm. Length; ±1.0 mm. | 6.Product Photo DXL-WS SERIES. 7.SECTIONVIEW DXL-WS PROFILE. 8. PACKAGING Standard bundle packing category-name printed bag. Easy for storage and identification |
| --- | --- |

Specification Table

| Model | Web （A）mm | Flange（B）mm | Thickness（T）mm | Length (L) mm | Packing |
| --- | --- | --- | --- | --- | --- |
| DXL-WS64 | 64 | 35 | 0.40 - 0.60 mm | 2800 3000 custom（≥1000） | As per order confirmation |
| DXL-WS73 | 73 | 32 | 0.40 - 0.60 mm | 2800 3000 custom（≥1000） | As per order confirmation |
| DXL-WS92 | 95 | 35 | 0.40 - 0.60 mm | 2800 3000 custom（≥1000） | As per order confirmation |

Notes

- Custom length available for all models

- Special dimensions and thickness are available upon request

- Theoretical weight is for reference only. Actual weight shall prevail