Publication Date 2025

| DXL STEEL FRAMING SYSTEMS PRODUCT DATA SHEET |  |
| --- | --- |

DRYWALL STUD

| DXL-WS-SERIES DXL Drywall Studs are cold-formed steel sections used in non-load bearing drywall framing systems. DXL 竖向龙骨采用优质冷轧镀锌钢板成型，用于非承重隔墙系统。 1. PRODUCT INFORMATION / 产品信息 Product Name 产品名称; Drywall Stud 竖向龙骨. Model No. 型号; DXL-WS Series. Category 类别; Drywall Framing System. Application 应用; Interior Partition Walls. 2. DIMENSIONS / 尺寸参数 Web Width (A); 64 73 92 100 150 mm. Thickness (T); 0.4 0.5 0.6 mm. Length; 2800 / 3000 / Custom（≥2000）. 3. MATERIAL / 材料与表面处理 Material材质; Galvanized steel. Zinc Coating 镀锌层; Z100 - Z275 g/m². Surface finish 表面处理; Hot-dip Galvanized. 4. TOLERANCE / 公差标准 Thickness 厚度公差; ±0.03 mm. Width 宽度公差; ±0.50 mm. Length 长度公差; ±5.0 mm. | 6.Product Photo / 产品实物 DXL-WS SERIES. 7.SECTIONVIEW / 截面图 DXL-WS PROFILE. 8. PACKAGING / 包装示意 Standard bundle packing category-name printed bag. Easy for storage and identification |
| --- | --- |

For Sales Inquiries, please contact our global support team via WhatsApp:＋78764422 or dxlmetal@gmail.com

DXL—Reliable Quality，Global Trust

Specification Table

| Model | Web （A）mm | Flange（B）mm | Thickness（T）mm | Length (T) mm |
| --- | --- | --- | --- | --- |
| DXL-WS64 | 64 | 35 | 0.4 0.5 0.6 | 2800 3000 custom（≥2000） |
| DXL-WS73 | 73 | 32 | 0.4 0.5 0.6 | 2800 3000 custom（≥2000） |
| DXL-WS92 | 95 | 35 | 0.4 0.5 0.6 | 2800 3000 custom（≥2000） |
| DXL-WS100 | 100 | 45 | 0.4 0.5 0.6 | 2800 3000 custom（≥2000） |
| DXL-WS150 | 150 | 32 | 0.4 0.5 0.6 | 2800 3000 custom（≥2000） |

Notes

- Custom length available for all models

- Special dimensions and thickness are available upon request

For Sales Inquiries, please contact our global support team via WhatsApp:＋78764422 or dxlmetal@gmail.com

DXL—Reliable Quality，Global Trust