Publication Date 2025

| DXL STEEL FRAMING SYSTEMS PRODUCT DATA SHEET |  |
| --- | --- |

DRYWALL TRACK

| DXL-WT-SERIES DXL Tracks are cold-formed galvanized steel sections used as top and bottom channels in non-load bearing drywall partition systems. 1. PRODUCT INFORMATION Product Name; Drywall Track. Model No.; Drywall WT Series. Category; Drywall Framing System. Application; Partition wall top and bottom track systems. 2. DIMENSIONS Web Width (A); 65 75 94 130. Thickness (T); 0.40 - 0.60 mm. Length; 2800 / 3000 / Custom（≥2000）. 3. MATERIAL Material; Hot-dip Galvanized steel. Zinc Coating; Z100 - Z275 g/m². Surface finish; Galvanized silver-grey finish; custom color powder coating available.. 4. TOLERANCE Thickness; 0/-0.02 mm. Width; 0/-0.5 mm. Length; ±1.0 mm. | 6.Product Photo DXL-WT SERIES. 7.SECTIONVIEW DXL-WS PROFILE. 8. PACKAGING Standard bundle packing category-name printed bag. Easy for storage and identification |
| --- | --- |

Specification Table

| Model | Web （A）mm | Flange（B）mm | Thickness（T）mm | Length (T) mm | Packing |
| --- | --- | --- | --- | --- | --- |
| DXL-WT-65 | 65 | 26 | 0.40 - 0.60 mm | 2800 3000 custom（≥2000） | As per order confirmation |
| DXL-WT-75 | 75 | 35 | 0.40 - 0.60 mm | 2800 3000 custom（≥2000） | As per order confirmation |
| DXL-WT-94 | 94 | 32 | 0.40 - 0.60 mm | 2800 3000 custom（≥2000） | As per order confirmation |

Notes

- Custom length available for all models

- Special dimensions and thickness are available upon request

- Theoretical weight is for reference only. Actual weight shall prevail